## Slide 1: GUITAR – Graphene from the UI Thermolyzed Asphalt Reaction
The Scientific Method at Work
Chem 409, 2017

## Slide 2: Scientific Method
Observation/Discovery
Hypothesis
Experiments
Conclusions
How is this done?
Is it this clean?

## Slide 3: Discovery
Metals Analysis of Piceance Basin Oil Shale
Sample Pyrolyzed to Remove Organics
WY
ID
UT
CO
Piceance Basin

## Slide 4
University of Idaho Thermolyzed Asphalt Reaction

## Slide 6: GUITAR and Graphites/Graphenes
Source: Wikipedia
Graphene
sp2 Carbon

## Slide 7
Basal Plane
Edge Plane
Morphology
  Basal Plane
  Edge Plane
Graphene
Graphite

## Slide 8: Scientific Method
Observation/Discovery
Hypothesis
  It’s Graphene (or a very thin graphite)
  Graphene 2010 Nobel Prize in Physics
  Graphene is difficult to synthesize
Experiments
Conclusions

## Slide 9: Scientific Method
Observation/Discovery
Hypothesis
Experiments
  Physical and Chemical Analyses (Characterization)
  Scanning Electron Microscopy
Conclusions

## Slide 10: Physical Characterization
XPS
sp2 Carbon
532 nm laser
Raman
IR
Disordered
Graphite
Intra-graphene
Stretches

## Slide 11
Scanning Electron Micrographs

## Slide 12
Photographs of Basal Planes
Scanning Electron Micrographs

## Slide 13: Physical Characterization
 | Graphite/Graphene | GUITAR | Other Notes
XPS | sp2 carbon | sp2 carbon | Similar
Raman | Crystalline | Nanocrystalline | GUITAR may be disordered graphene
Microscopy -Optical -Electron | Layers | Layers | Similar

## Slide 14: Scientific Method
Observation/Discovery
Hypothesis
Experiments
Conclusions
  It’s Graphene!
  Publication
  Patent w/UI

## Slide 16: What Next?
GUITAR = Graphene (or a very thin graphite)
Graphene hypothesized to have extraordinary properties
Let’s Make Electrodes Out of GUITAR.

## Slide 17: Measure Rates of Electron Transfer
Why?
Batteries
Fuel Cells
Solar Cells
Sensors
Ultracapacitors
Anodic Water Purification
GUITAR Electrode
e-
Ox
Red
Aqueous
Solution

## Slide 18: GUITAR Electrode

## Slide 19: Redox Probes
Fe(CN)63- + e- ⇄ Fe(CN)64-
Ru(NH3)63+ + e- ⇄ Ru(NH3)62+
Source: Wikipedia
k0
k0

## Slide 20
GUITAR Electrode
3-
4-
e-
(Ox)
(Red)
Aqueous Solution

## Slide 21
k0 cm/s | Fe(CN)6 3-/4- | Ru(NH3)6 3+/2+
GUITAR | 1.2 × 10-2 | 1.7 × 10-2
k0 obtained from Cyclic Voltammetry
Conclusion: GUITAR has fast heterogeneous electron transfer

## Slide 22: What Next?
Publish in Literature
  Graphene is great stuff
Better Read What’s Going On in Literature

## Slide 23
HOPG, McCreery, Anal. Chem. 1992, 64, 2518-2524

## Slide 24: Density of Electronic States
σ+
π+
σ-
π-
EFermi
DOS
EFermi
Energy (eV)
Crystalline Graphite
Disordered Graphite
McCreery et al, J. Phys. Chem. 1994, 98, 5314-5319
Valence
Band
Conduction
Band

## Slide 25: e- Transfer Rates Edge vs. Basal Planes
Electron transfer rates on HOPG, graphites and graphenes
  Anisotropic Behavior
  Edge Plane >> Basal Plane
Edge
Basal
slow
Ox + ne-
Red
Fast
Ox + ne-
Red
McCreery et al, J. Phys. Chem. 1994, 98, 5314-5319

## Slide 26: Step Defects
Basal Plane
Edge Plane
Step Defect
Fast e- transfer too
Fast
Ox + ne-
Red

## Slide 27
k0 cm/s | Fe(CN)6 3-/4- | Ru(NH3)6 3+/2+ | 
BP-GUITAR | 1.2 × 10-2 | 1.7 × 10-2 | This work
EP-GUITAR | 3 × 10-2 | -- | 
Basal Plane Materials |  |  | 
BP-Graphene |  10-9 |  10-3 | Literature
BP-HOPG |  10-6 |  | 
BP-Graphite |  10-3 |  | 
Edge Plane Materials |  |  | 
EP-Graphene |  10-2 | -- | Literature
EP-HOPG |  |  10-1 | 
EP-Graphite |  |  10-2 | 
Glassy Carbon |  |  10-2 | 
k0 obtained from Cyclic Voltammetry
No Anisotropy
EP = BP
Anisotropy
EP >> BP

## Slide 28: Scientific Method
Observation/Discovery
Hypothesis
Experiments
Conclusions
  It’s Graphene!
  Publication
  Patent w/UI

## Slide 29: Scientific Method
Observation/Discovery
  GUITAR has fast e- transfer
    Basal Plane = Edge Plane
  Graphene and Graphites (1990’s to 2011)
    Edge Plane >> Basal Plane
Hypothesis
Experiments
Conclusions
(glad I didn’t publish so quickly)

## Slide 30: Scientific Method
Observation/Discovery
  What Else is Different About GUITAR?
Hypothesis
Experiments
Conclusions

## Slide 31: Electrochemical Window
Anodic Limit
  Water breakdown
    2H2O  O2 + 4H+ + 4e- E0 = 1.23 volts
  Corrosion
    C + 2H2O  CO2 + 4H+ + 4e- E0 = 0.207 V
Cathodic Limit
  Water breakdown
    4H+ + 4e-  2H2 E0 = 0.00 volts

## Slide 32
E, potential (Volts)
More oxidizing
Current
1.23 V
Oxygen overpotential
0 V
Hydrogen
overpotential
No reaction
2H2O  O2 + 4H+ + 4e-
4H+ + 4e-  2H2
1 M strong acid

## Slide 33: Potential Windows in 1 M H2SO4

## Slide 34: Summary Potential Windows in 1 M H2SO4
Material | Current Limits (µA/cm2) | Cathodic limits (V) | Anodic limits (V) | Total Windows (V) | Reference
GUITAR | 200 | -0.9 | 2.1 | 3 | This work
Graphites | 200 | -0.4 to -0.5 | 1.4 to 1.9 | 2 | This work & Literature
Boron Doped Diamond Diamond-Like Carbon Amorphous Carbons | 200 – 300 | -0.4 to -1.25 | 1.7 to 2.4 | 3 | Literature

## Slide 35: Observations
GUITAR has resistance to corrosion
  GUITAR = Synthetic Diamonds ($$)
  GUITAR > Graphene or Graphite
  GUITAR is sp2 carbon
  Diamonds are sp3

## Slide 36: Scientific Method
Observation/Discovery
  What Else is Different About GUITAR?
  GUITAR has fast e- transfer
    Basal Plane = Edge Plane
  Resistance to Corrosion > Graphene/Graphite
Hypothesis
  GUITAR is not Graphene or Graphite!
Experiments
Conclusions

## Slide 37: Scientific Method
Observation/Discovery
Hypothesis
  GUITAR is not Graphene or Graphite!
  New Allotrope?
Experiments
Conclusions

## Slide 38: Scientific Method
Observation/Discovery
  What Else is Different About GUITAR?
  Resistance to Corrosion > Graphene/Graphite
Hypothesis
  GUITAR is not Graphene or Graphite!
  New Allotrope?
  Why is GUITAR Resistant to Corrosion?
Experiments
Conclusions

## Slide 39: Potential Windows in 1 M H2SO4

## Slide 40
Murray et al, Analytical Chemistry, 1995, 67, 2201-2206
Diagnostic from Cyclic Voltammetric Sweeps
Electrolyte inter- and de-intercalation
  [Cx] + [HSO4-] + y H2O ⇄ [Cx+ HSO4-]y(H2O) + e-
Blister formation on graphitic anodes
Electrolyte Intercalation
Gas Evolution
Blister Formation
Pit Corrosion
CO2(g) + O2(g)
HSO4-
Step Defect
Grain
Boundary
HSO4-

## Slide 41
CO2(g) + O2(g)
HSO4-
Step Defect
Grain
Boundary
HSO4-
HSO4-
+ + + + + +
HSO4-
HSO4-
HSO4-
HSO4-
HSO4-
+ + +
HSO4-
HSO4-
HSO4-

## Slide 42: GUITAR Lacks Voltammetric Evidence for Electrolyte Intercalation
De-intercalation peak current
GUITAR
Pyrolytic Graphite
Potential vs. Ag/AgCl
Zero De-intercalation current
1 M H2SO4
    [Cx+ HSO4-]y(H2O) + e-  [Cx] + [HSO4-] + y H2O
Intercalation peak current

## Slide 43: What about edge plane intercalation?
HSO4-
335 pm
Electrolyte Intercalation
Edge plane
Electrodes

## Slide 44
Edge Plane Graphite
Edge Plane GUITAR

## Slide 45: Observations
CO2(g) + O2(g)
HSO4-
Step Defect
Grain
Boundary
HSO4-
Graphite
GUITAR
Impervious to Intercalation

## Slide 46: Scientific Method
Observation/Discovery
  GUITAR does not allow for electrolyte intercalation
Hypothesis
  ?
Experiments
Conclusions

## Slide 47: Scientific Method
Observation/Discovery
  Collect More Observations
Hypothesis
  ?
Experiments
Conclusions

## Slide 48
Photographs of Basal Planes
Scanning Electron Micrographs
Graphite Morphology

## Slide 49: What’s Going on at The Basal Planes?
What’s so different about GUITAR’s basal planes?
  Disordered Graphite?
Went back at looked old scanning electron micrographs.

## Slide 50: GUITAR and Graphites/Graphenes
Shared Morphology
Basal Plane
Edge Plane
  Step Defects?
    Not Observed on GUITAR
GUITAR

## Slide 51: GUITAR Lacks Steps Defects
GUITAR – Lacks Step Defects
HOPG – Step Defects

## Slide 52
AFM Asylum Research – Spring 2016 ACS Meeting San Diego – On Quartz
Line Section
GUITAR
Graphite (HOPG)

## Slide 53: AFM Studies of Basal Planes
GUITAR
  Lacks Step Defects
  Rougher Surfaces 10-50 nm Amplitudes
HOPG
  Relatively Flat, 2-4 nm Amplitudes
  Clear Step Defects

## Slide 54: Scientific Method
Observation/Discovery
  Collect More Observations
  AFM and SEM indicate no Step Defects
Hypothesis
  GUITAR is a new allotrope of Carbon
  Atomic Arrangement?
Experiments
Conclusions

## Slide 55: GUITAR – Which Allotrope?
Fullerenes, 1996
Nobel Prize
Curl, Kroto, Smalley
Carbon nanotubes
1991
Amorphous carbon
Diamond
Graphite
Lonsdaleite
1968
Glassy Carbon
http://en.wikipedia.org/wiki/Carbon

## Slide 56: Scientific Method
Observation/Discovery
Hypothesis
  GUITAR is a new allotrope of Carbon
Experiments
  Raman Spectroscopy w/ Boise State
  X-ray Diffraction w/ Texas A&M
Conclusions
  ?

## Slide 57: Scientific Method
Observation/Discovery
Hypothesis
Experiments
Conclusions
How is this done?

## Slide 58: What is it Good For?
GUITAR Applications
  Sensors (w/ Industry)
  Fuel Cells
    One of the Highest Performers
  Batteries
    Redox Flow – One of the Highest Performers (Published)
  Water Purification
    Anodic Purification (in place of diamond ($$))
    Desalinization
  Chromatography
    New Station Phases