## Slide 1: CAD Design for Manufacturing
Basic Considerations for Machining vs. 3D Printing

## Slide 2: FDM 3D Printer Anatomy

## Slide 3: Mill vs. Lathe vs. FDM printing

## Slide 4: Major Differences
Process: Subtractive vs. Additive mfg.
Time: small parts print "fast" (min-hrs), large parts print slow (hrs-days). Machining time depends on amount of material removal and number/complexity of part features (hours)
Cost: printing depends on material used; machining depends mostly on time and number of setups required. Most filaments are cheap.
Strength/Rigidity: PLA, ABS, Nylon, Onyx, Onyx w/ CF reinf., 6061-T6
Precision: Printing +/- 0.1mm (~0.005") in X-Y plane, similar in Z (if support isn't needed and warping is minimized).
Geometry limitations:
  X-Y tensile strength is almost double of inter-layer strength
  Machining pockets can't have square internal corners!

## Slide 5: Design for Machining
Basic Tips/Considerations

## Slide 6: Tools are Round (internal pockets have radii)

## Slide 7: Rules of thumb
Tool OD:Length ratio should stay > 1:4 for milling (for deflection & chatter) --> may require multiple passes
Small radii tools:
  can't cut as deep
  take longer to remove material
Only include number of significant figures needed --> zeros cost $
  Example for a small part
    0.05-0.1 inches (1-2 mm) when precision/weight doesn't matter
    0.01 inches (0.2 mm) for low precision
    0.005 inches (0.1 mm) for moderate precision
    0.0005-0.001 inches (0.01-0.02 mm) for high precision

## Slide 8: Design for FDM
3D Printing Basics

## Slide 9: Methods of Printing
Extrusion: aka Fused Deposition Modeling (FDM)
Inkjet
Selective Laser Sintering (SLS)
Stereolithography (SLA)

## Slide 10: FDM 3D Printer Anatomy

## Slide 11: Hotend Assembly Anatomy
Filament OD = 1.75 mm
Nozzle extrusion width = 0.4 mm
Extruder gears are often separated from the hotend by a Bowden cable
  Pros:
  reduces weight being moved
  allows faster print speeds
  Cons:
  adds compliance to the filament
  more difficult to print flexible filament

## Slide 12: Limitations that influence design
Print volume (aka "build volume")
Bed adhesion
Layer adhesion
Support material
Print directionality
Feature size
MarkForged Onyx Pro
MarkForged MarkTwo
Sindoh 2X
Sindoh 3DWOX1
Bambu Lab X1 Carbon (w/ 4-spool AMS)

## Slide 13: Build Volume
 | DP200/3DWOX1 | 2X | OnyxPro / MarkTwo | X1 Carbon
Build Volume | 210 x 200 x 195 mm | 228 x 200 x300 mm | 320 x 132 x 154 mm | 256 x 256 x 256
Layer Height | 0.050 - 0.2 mm | 0.050 - 0.2 mm | 0.1 - 0.2 mm | 0.1 mm
Materials | DP200: PLA/ABS 3DWOX1: PLA/ABS/ other non-Sindoh | PLA/ABS/TPU/PVA (other non-sindoh) | Onyx/Nylon MarkTwo only: Cont. fiber reinforcement (Carbon Fiber, Fiber Glass, HSHT Fiber Glass, Kevlar) | PLA/ABS/PETG/ASA/TPU/NA/NACF/… lots

## Slide 14: Bed Adhesion
Prevent inadvertent separation
Reduce warping
3 types
  Raft – stabalize models with small footprint
  Brim – add stability that's easy to remove
  Skirt – prime nozzle for steady flow
Cons: rafts can be hard to remove and add significant print time
Recommendation: design parts with flat surface in contact with bed and avoid use of rafts when possible

## Slide 15: Layer Adhesion
Affected by:
  Hot end clogs
  Print speed
  Hot end temp
  Filament feed rate
  Part cooling
  Layer height
  Moisture in filament
  Nozzle width

## Slide 16: Support Material
Purpose: prevent sagging of filament before it has time to cool.
Cons:
  Causes roughness on underside of overhangs
  Hard to remove from interior or small spaces
Cleanest prints don't use it
  Not needed for angles >45 degrees (sometimes down to 30 degrees)
  Design your part to have only minimal and short lengths of overhangs <45 deg from horizontal (when possible)
  If not avoidable, consider PVA or play with the new supports in the prusa slicer.

## Slide 17: Effects of Print Directionality
X/Y plane
  Smooth curves (high resolution apperance)
  Continuous plastic (high strength)
Z/X and Z/Y planes
  Layer height and support material determine smothness of arcs/lines
  Weaker along layer lines
All planes
  Unsupported material will be affected by gravity in the Z-direction
  Larger layer height will be affected less by gravity

## Slide 18: New in Cura and Prusaslicer

## Slide 19: Feature Size
Nozzle is 0.4 mm
Can't make features smaller than that
Preferable at least 2 x nozzle width (~ > 1 mm)
https://support.xometry.com/hc/en-us/articles/217723698-What-is-the-smallest-feature-that-you-can-print-

## Slide 20: How do you print a part?
Make a part in SolidWorks
Export part as an STL (using "save-as")
Import (or drag and drop) STL into slicer
Select printer and material settings
Adjust print settings or use default ("Normal" from Easy Mode)
Build layers ("Layer Viewer" in 3DWOX Desktop)
File-->Save G-Code to flash drive
Put flash drive into printer’s USB port
Select "Print", Select your file, and follow on-screen instructions
Remove your flash drive when small “x” goes away from on-screen usb icon

## Slide 21: 3D Printing Resources
Overview
  3D Printing - Mindworks (shoutwiki.com)
Troubleshooting
  Print Quality Guide (simplify3d.com)
Strength vs. print quality of prints
  https://www.youtube.com/watch?v=Bl2ESvtBiLo
  Less cooling = lower print accuracy but higher inter-layer bond strength