## Slide 1
MATERIAL SELECTION GUIDE
 | Machinability | Weldability | Tensile Strength | Heat Treatable | Hardness | Rust | Cost | Size of Stock Priced
Cold Drawn Steel | * |  |  |  |  |  |  | 
1018 | 62% | EASY | 64 ksi | YES | 167 HB | Yes | $27 | 1”x2”x12”
1213 | 136% | POOR | 78 ksi | YES | 39 HRC | Yes |  | 
12L14 | 170% | POOR | 78 ksi | YES | 84 HRB | Yes | $16 | 1"x1"x12"
1117/11L17 | 91% | POOR | 69 ksi | YES | 156 HB | Yes |  | 
Hot Rolled Steel |  |  |  |  |  |  |  | 
A36 | 72% | EASY | 58-79.8 ksi | YES | 149 HB | Yes | $70 | 1”x2”x12”
1040 | 64% | EASY | 86 ksi | YES | 201 HRB | Yes |  | 
1117 | 91% | POOR | 62 ksi | YES | 170 HRB | Yes | $10 | 1"DIAM x 12"
Steel Alloys |  |  |  |  |  |  |  | 
4130 | 72% | VERY EASY | 97 ksi | YES | 217 HRB | Yes | $16 | 1"DIAM x 12"
4140 | 66% | EASY | 148 ksi | YES | 40 HRC | Yes | $38 | 1”x2”x12”
4340 | 57% | FAIR | 185 ksi | YES | 93 HRB | Yes | $35 | ¼”x12”x12”
6150 | 60% | DIFFICULT | 136 ksi | YES | 45 HRC | Yes |  | 
8620 | 66% | EASY | 91.8 ksi | YES | 71 HRB | Yes | $42 | 2" DIAM x 12"
Stainless Steel |  |  |  |  |  |  |  | 
302 | 45% | EASY | 75 ksi | No | 92 HRB | No |  | 
303s/303se | 78% | FAIR | 90 ksi | No | 96 HRB | No |  | 
304 | 45% | EASY | 75 ksi | Yes | 92 HRB | No | $65 | 1”x2”x12”
316 | 45% | EASY | 75 ksi | Solution Treatment only | 95 HRB | No | $100 | 1”x2”x12”
440C | 40% | POOR | 110 ksi | Yes | 269 HB | No | $120 | 1”x2”x12”
17-4 | 48% | GOOD | 150 ksi | Solution Treatment only | 331 HB | No | $83 | 1”x2”x12”
Aluminum | ** |  |  |  |  |  |  | 
2024 T3 | 90% | POOR | 70 ksi | No | 120 HB | No | $50 | 1”x2”x12”
5052 H32 | 88% | GOOD | 33 ksi | No | 60 HB | No | $55 | ½”x12”x12”
6061 T6 | 90% | GOOD | 45 ksi | Yes | 95 HB | No | $19 | 1”x2”x12”
7075 T6 | 80% | POOR | 83 ksi | Yes | 150 HB | No | $48 | 1”x2”x12”
* All Steels are rated with a percent machinability with reference to 1212 as being 100%
** All Aluminums are rated with a percent machinability with reference to 2011 as being 100%